Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Oxygen | 64.416 | 0.529 | 81.234 |
| Magnesium | 2.614 | 0.146 | 2.169 |
| Calcium | 32.970 | 0.498 | 16.597 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Oxygen | 50.387 | 1.178 | 71.326 |
| Magnesium | 1.745 | 0.174 | 1.626 |
| Calcium | 47.868 | 1.145 | 27.048 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Oxygen | 42.173 | 0.910 | 60.212 |
| Magnesium | 18.480 | 0.409 | 17.363 |
| Calcium | 39.347 | 0.687 | 22.425 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Oxygen | 44.492 | 1.002 | 65.993 |
| Magnesium | 2.974 | 0.191 | 2.902 |
| Calcium | 52.535 | 0.959 | 31.105 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Oxygen | 14.950 | 1.769 | 30.461 |
| Magnesium | 0.691 | 0.131 | 0.926 |
| Calcium | 84.359 | 1.759 | 68.613 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 7

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Oxygen | 23.136 | 1.476 | 42.498 |
| Magnesium | 2.401 | 0.177 | 2.902 |
| Calcium | 74.463 | 1.439 | 54.600 |