Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 8.798 | 0.182 | 24.933 |
| Niobium | 91.202 | 0.182 | 75.067 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 8.866 | 0.187 | 25.093 |
| Niobium | 91.134 | 0.187 | 74.907 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  19.8 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 8.881 | 0.190 | 25.127 |
| Niobium | 91.119 | 0.190 | 74.873 |