Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 491.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

All spectra (displaying atomic %)

| Name | Al | Nb |
| --- | --- | --- |
| Spectrum 1 | 26.227 | 73.773 |
| Spectrum 2 | 26.296 | 73.704 |
| Spectrum 3 | 26.469 | 73.531 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 8.655 | 0.177 | 24.599 |
| Niobium | 91.345 | 0.177 | 75.401 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 8.022 | 0.174 | 23.096 |
| Niobium | 91.978 | 0.174 | 76.904 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 9.346 | 0.187 | 26.199 |
| Niobium | 90.654 | 0.187 | 73.801 |