Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 11.998 | 0.208 | 31.946 |
| Niobium | 88.002 | 0.208 | 68.054 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 12.127 | 0.208 | 32.213 |
| Niobium | 87.873 | 0.208 | 67.787 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 11.964 | 0.208 | 31.878 |
| Niobium | 88.036 | 0.208 | 68.122 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 71.196 | 0.826 | 89.486 |
| Niobium | 28.804 | 0.826 | 10.514 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 61.207 | 0.959 | 84.454 |
| Niobium | 38.793 | 0.959 | 15.546 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 11.989 | 0.221 | 31.928 |
| Niobium | 88.011 | 0.221 | 68.072 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 7

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 13.271 | 0.227 | 34.507 |
| Niobium | 86.729 | 0.227 | 65.493 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 8

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 11.793 | 0.218 | 31.523 |
| Niobium | 88.207 | 0.218 | 68.477 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 491.9 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

All spectra (displaying atomic %)

| Name | Al | Nb |
| --- | --- | --- |
| Spectrum 1 | 32.195 | 67.805 |
| Spectrum 2 | 31.631 | 68.369 |
| Spectrum 3 | 32.363 | 67.637 |