Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 491.9 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 29.029 | 0.381 | 58.478 |
| Niobium | 70.971 | 0.381 | 41.522 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 491.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 28.970 | 0.387 | 58.409 |
| Niobium | 71.030 | 0.387 | 41.591 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 491.9 µm

Acquisition conditions

Acquisition time (s)  20.2 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 28.848 | 0.379 | 58.265 |
| Niobium | 71.152 | 0.379 | 41.735 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 41.606 | 0.509 | 71.043 |
| Niobium | 58.394 | 0.509 | 28.957 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 41.914 | 0.518 | 71.302 |
| Niobium | 58.086 | 0.518 | 28.698 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 42.012 | 0.526 | 71.385 |
| Niobium | 57.988 | 0.526 | 28.615 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 25.610 | 0.377 | 54.241 |
| Niobium | 74.390 | 0.377 | 45.759 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 25.693 | 0.384 | 54.349 |
| Niobium | 74.307 | 0.384 | 45.651 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Aluminum | 25.641 | 0.386 | 54.283 |
| Niobium | 74.359 | 0.386 | 45.717 |