Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 28.197 | 0.485 | 40.791 |
| Zirconium | 71.803 | 0.485 | 59.209 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 29.666 | 0.490 | 42.528 |
| Zirconium | 70.334 | 0.490 | 57.472 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 28.424 | 0.471 | 41.061 |
| Zirconium | 71.576 | 0.471 | 58.939 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 49.939 | 0.606 | 63.637 |
| Zirconium | 50.061 | 0.606 | 36.363 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 48.337 | 0.576 | 62.141 |
| Zirconium | 51.663 | 0.576 | 37.859 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 51.069 | 0.607 | 64.677 |
| Zirconium | 48.931 | 0.607 | 35.323 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 3.655 | 0.274 | 6.239 |
| Zirconium | 96.345 | 0.274 | 93.761 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 3.401 | 0.270 | 5.817 |
| Zirconium | 96.599 | 0.270 | 94.183 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 3.322 | 0.276 | 5.686 |
| Zirconium | 96.678 | 0.276 | 94.314 |