Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 50.250 | 0.557 | 63.925 |
| Zirconium | 49.750 | 0.557 | 36.075 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 50.921 | 0.565 | 64.542 |
| Zirconium | 49.079 | 0.565 | 35.458 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 49.693 | 0.556 | 63.409 |
| Zirconium | 50.307 | 0.556 | 36.591 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 8

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 32.919 | 0.508 | 46.264 |
| Zirconium | 67.081 | 0.508 | 53.736 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 2.626 | 0.257 | 4.518 |
| Zirconium | 97.374 | 0.257 | 95.482 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 2.343 | 0.256 | 4.038 |
| Zirconium | 97.657 | 0.256 | 95.962 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 31.887 | 0.525 | 45.095 |
| Zirconium | 68.113 | 0.525 | 54.905 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 34.176 | 0.534 | 47.668 |
| Zirconium | 65.824 | 0.534 | 52.332 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 3.642 | 0.285 | 6.218 |
| Zirconium | 96.358 | 0.285 | 93.782 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 42.461 | 0.579 | 56.420 |
| Zirconium | 57.539 | 0.579 | 43.580 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 42.312 | 0.558 | 56.270 |
| Zirconium | 57.688 | 0.558 | 43.730 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 43.156 | 0.554 | 57.116 |
| Zirconium | 56.844 | 0.554 | 42.884 |