Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 48.942 | 0.507 | 62.709 |
| Zirconium | 51.058 | 0.507 | 37.291 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 49.084 | 0.503 | 62.843 |
| Zirconium | 50.916 | 0.503 | 37.157 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 47.986 | 0.492 | 61.811 |
| Zirconium | 52.014 | 0.492 | 38.189 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 49.852 | 0.529 | 63.557 |
| Zirconium | 50.148 | 0.529 | 36.443 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 50.014 | 0.531 | 63.707 |
| Zirconium | 49.986 | 0.531 | 36.293 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 49.198 | 0.534 | 62.949 |
| Zirconium | 50.802 | 0.534 | 37.051 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 33.166 | 0.484 | 46.541 |
| Zirconium | 66.834 | 0.484 | 53.459 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 33.732 | 0.487 | 47.175 |
| Zirconium | 66.268 | 0.487 | 52.825 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 35.637 | 0.492 | 49.274 |
| Zirconium | 64.363 | 0.492 | 50.726 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 7

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 13.145 | 0.357 | 20.980 |
| Zirconium | 86.855 | 0.357 | 79.020 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 8

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 17.296 | 0.390 | 26.842 |
| Zirconium | 82.704 | 0.390 | 73.158 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 131.2 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 12.567 | 0.365 | 20.138 |
| Zirconium | 87.433 | 0.365 | 79.862 |