Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 57.553 | 0.579 | 70.403 |
| Zirconium | 42.447 | 0.579 | 29.597 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 56.522 | 0.573 | 69.518 |
| Zirconium | 43.478 | 0.573 | 30.482 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 57.770 | 0.569 | 70.588 |
| Zirconium | 42.230 | 0.569 | 29.412 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 52.723 | 0.581 | 66.176 |
| Zirconium | 47.277 | 0.581 | 33.824 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 52.279 | 0.580 | 65.776 |
| Zirconium | 47.721 | 0.580 | 34.224 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 52.282 | 0.578 | 65.779 |
| Zirconium | 47.718 | 0.578 | 34.221 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 68.506 | 0.592 | 79.236 |
| Zirconium | 31.494 | 0.592 | 20.764 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 68.473 | 0.586 | 79.211 |
| Zirconium | 31.527 | 0.586 | 20.789 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 68.558 | 0.590 | 79.276 |
| Zirconium | 31.442 | 0.590 | 20.724 |