Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 79.774 | 0.510 | 87.373 |
| Zirconium | 20.226 | 0.510 | 12.627 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 80.364 | 0.496 | 87.775 |
| Zirconium | 19.636 | 0.496 | 12.225 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 80.533 | 0.477 | 87.890 |
| Zirconium | 19.467 | 0.477 | 12.110 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 9

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 64.971 | 0.540 | 76.492 |
| Zirconium | 35.029 | 0.540 | 23.508 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 8

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 64.069 | 0.546 | 75.776 |
| Zirconium | 35.931 | 0.546 | 24.224 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 7

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 65.827 | 0.536 | 77.166 |
| Zirconium | 34.173 | 0.536 | 22.834 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 53.645 | 0.534 | 67.000 |
| Zirconium | 46.355 | 0.534 | 33.000 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 52.147 | 0.529 | 65.657 |
| Zirconium | 47.853 | 0.529 | 34.343 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 97.935 | 0.357 | 98.812 |
| Zirconium | 2.065 | 0.357 | 1.188 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 98.234 | 0.362 | 98.985 |
| Zirconium | 1.766 | 0.362 | 1.015 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 98.237 | 0.354 | 98.987 |
| Zirconium | 1.763 | 0.354 | 1.013 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Chromium | 53.581 | 0.547 | 66.942 |
| Zirconium | 46.419 | 0.547 | 33.058 |