Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.708 | 0.421 | 50.398 |
| Nickel | 67.292 | 0.421 | 49.603 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.310 | 0.418 | 49.945 |
| Nickel | 67.689 | 0.418 | 50.055 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.177 | 0.413 | 49.792 |
| Nickel | 67.823 | 0.413 | 50.208 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 98.308 | 0.302 | 99.184 |
| Nickel | 1.692 | 0.302 | 0.816 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 98.267 | 0.288 | 99.164 |
| Nickel | 1.733 | 0.288 | 0.836 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 98.338 | 0.292 | 99.198 |
| Nickel | 1.662 | 0.292 | 0.802 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 46.318 | 0.491 | 64.332 |
| Nickel | 53.682 | 0.491 | 35.668 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 47.200 | 0.498 | 65.140 |
| Nickel | 52.800 | 0.498 | 34.860 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 46.647 | 0.492 | 64.634 |
| Nickel | 53.353 | 0.492 | 35.366 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.2 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 56.945 | 0.494 | 73.438 |
| Nickel | 43.055 | 0.494 | 26.562 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 56.921 | 0.536 | 73.419 |
| Nickel | 43.079 | 0.536 | 26.581 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 57.365 | 0.568 | 73.771 |
| Nickel | 42.635 | 0.568 | 26.229 |