Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 78.7 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.040 | 0.356 | 49.636 |
| Nickel | 67.960 | 0.356 | 50.364 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 78.7 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 31.964 | 0.354 | 49.548 |
| Nickel | 68.036 | 0.354 | 50.452 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 78.7 µm

Acquisition conditions

Acquisition time (s)  30.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 31.782 | 0.355 | 49.338 |
| Nickel | 68.218 | 0.355 | 50.662 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 65.6 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 45.468 | 0.531 | 63.542 |
| Nickel | 54.532 | 0.531 | 36.458 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 65.6 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 44.326 | 0.516 | 62.466 |
| Nickel | 55.674 | 0.516 | 37.534 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 65.6 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 44.969 | 0.531 | 63.075 |
| Nickel | 55.031 | 0.531 | 36.925 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 1.312 mm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 37.524 | 0.471 | 55.664 |
| Nickel | 62.476 | 0.471 | 44.336 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 1.312 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 37.424 | 0.494 | 55.559 |
| Nickel | 62.576 | 0.494 | 44.441 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 1.312 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.809 | 0.493 | 54.907 |
| Nickel | 63.191 | 0.493 | 45.093 |