Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.617 | 0.416 | 51.423 |
| Nickel | 66.383 | 0.416 | 48.577 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.747 | 0.423 | 51.568 |
| Nickel | 66.253 | 0.423 | 48.432 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.701 | 0.416 | 51.516 |
| Nickel | 66.299 | 0.416 | 48.484 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 46.151 | 0.485 | 64.177 |
| Nickel | 53.849 | 0.485 | 35.823 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 44.150 | 0.477 | 62.299 |
| Nickel | 55.850 | 0.477 | 37.701 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 46.278 | 0.483 | 64.295 |
| Nickel | 53.722 | 0.483 | 35.705 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 35.888 | 0.444 | 53.919 |
| Nickel | 64.112 | 0.444 | 46.081 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.405 | 0.445 | 54.476 |
| Nickel | 63.595 | 0.445 | 45.524 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 35.907 | 0.418 | 53.940 |
| Nickel | 64.093 | 0.418 | 46.060 |