Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 65.6 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.267 | 0.413 | 51.030 |
| Nickel | 66.733 | 0.413 | 48.970 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 65.6 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.529 | 0.422 | 51.324 |
| Nickel | 66.471 | 0.422 | 48.676 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 65.6 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.601 | 0.428 | 51.405 |
| Nickel | 66.399 | 0.428 | 48.595 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 39.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 24.586 | 0.366 | 40.529 |
| Nickel | 75.414 | 0.366 | 59.471 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 39.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 25.297 | 0.372 | 41.447 |
| Nickel | 74.703 | 0.372 | 58.553 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 39.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 26.067 | 0.375 | 42.430 |
| Nickel | 73.933 | 0.375 | 57.570 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 31.607 | 0.405 | 49.137 |
| Nickel | 68.393 | 0.405 | 50.863 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 31.220 | 0.415 | 48.688 |
| Nickel | 68.780 | 0.415 | 51.312 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 31.186 | 0.408 | 48.648 |
| Nickel | 68.814 | 0.408 | 51.352 |