Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 98.433 | 0.368 | 99.521 |
| Niobium | 1.567 | 0.368 | 0.479 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 97.896 | 0.381 | 99.355 |
| Niobium | 2.104 | 0.381 | 0.645 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 98.603 | 0.378 | 99.574 |
| Niobium | 1.397 | 0.378 | 0.426 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 37.033 | 0.438 | 66.050 |
| Niobium | 62.967 | 0.438 | 33.950 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.456 | 0.438 | 65.491 |
| Niobium | 63.544 | 0.438 | 34.509 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.699 | 0.444 | 65.727 |
| Niobium | 63.301 | 0.444 | 34.273 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.2 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 54.071 | 0.520 | 79.568 |
| Niobium | 45.929 | 0.520 | 20.432 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 53.391 | 0.588 | 79.120 |
| Niobium | 46.609 | 0.588 | 20.880 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 54.599 | 0.607 | 79.912 |
| Niobium | 45.401 | 0.607 | 20.088 |