Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 21.067 | 0.302 | 46.890 |
| Niobium | 78.933 | 0.302 | 53.110 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 20.009 | 0.293 | 45.279 |
| Niobium | 79.991 | 0.293 | 54.721 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 17.637 | 0.274 | 41.464 |
| Niobium | 82.363 | 0.274 | 58.536 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.191 | 0.428 | 65.231 |
| Niobium | 63.809 | 0.428 | 34.769 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 35.944 | 0.425 | 64.988 |
| Niobium | 64.056 | 0.425 | 35.012 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.551 | 0.437 | 65.584 |
| Niobium | 63.449 | 0.437 | 34.416 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  15.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.524 | 0.397 | 61.456 |
| Niobium | 67.476 | 0.397 | 38.544 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 31.092 | 0.391 | 59.881 |
| Niobium | 68.908 | 0.391 | 40.119 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.199 | 0.410 | 61.104 |
| Niobium | 67.801 | 0.410 | 38.896 |