Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 16.440 | 0.238 | 39.424 |
| Niobium | 83.560 | 0.238 | 60.576 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 16.545 | 0.235 | 39.606 |
| Niobium | 83.455 | 0.235 | 60.394 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 16.598 | 0.238 | 39.697 |
| Niobium | 83.402 | 0.238 | 60.303 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 26.462 | 0.320 | 54.345 |
| Niobium | 73.538 | 0.320 | 45.655 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 27.773 | 0.330 | 55.985 |
| Niobium | 72.227 | 0.330 | 44.015 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 7

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 28.063 | 0.333 | 56.340 |
| Niobium | 71.937 | 0.333 | 43.660 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 35.314 | 0.382 | 64.361 |
| Niobium | 64.686 | 0.382 | 35.639 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 35.085 | 0.387 | 64.130 |
| Niobium | 64.915 | 0.387 | 35.870 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 34.615 | 0.387 | 63.653 |
| Niobium | 65.385 | 0.387 | 36.347 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 1.093 mm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 19.751 | 0.276 | 44.878 |
| Niobium | 80.249 | 0.276 | 55.122 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 1.093 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 18.849 | 0.263 | 43.449 |
| Niobium | 81.151 | 0.263 | 56.551 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 1.093 mm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 18.242 | 0.251 | 42.464 |
| Niobium | 81.758 | 0.251 | 57.536 |