Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 14.372 | 0.219 | 35.700 |
| Niobium | 85.628 | 0.219 | 64.300 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 14.193 | 0.219 | 35.366 |
| Niobium | 85.807 | 0.219 | 64.634 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 14.440 | 0.224 | 35.826 |
| Niobium | 85.560 | 0.224 | 64.174 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 393.5 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 14.315 | 0.224 | 35.593 |
| Niobium | 85.685 | 0.224 | 64.407 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 6.632 | 0.158 | 19.026 |
| Niobium | 93.368 | 0.158 | 80.974 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 6.176 | 0.156 | 17.882 |
| Niobium | 93.824 | 0.156 | 82.118 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 6.257 | 0.154 | 18.085 |
| Niobium | 93.743 | 0.154 | 81.915 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 6.460 | 0.158 | 18.597 |
| Niobium | 93.540 | 0.158 | 81.403 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 8.526 | 0.167 | 23.567 |
| Niobium | 91.474 | 0.167 | 76.433 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 8.370 | 0.181 | 23.205 |
| Niobium | 91.630 | 0.181 | 76.795 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 8.437 | 0.184 | 23.361 |
| Niobium | 91.563 | 0.184 | 76.639 |