Spectrum details

Project	New project 	Spectrum name	Spectrum 10

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 13.846 | 0.267 | 22.571 |
| Vanadium | 86.154 | 0.267 | 77.429 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 9

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 13.527 | 0.269 | 22.102 |
| Vanadium | 86.473 | 0.269 | 77.898 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 8

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 13.618 | 0.265 | 22.236 |
| Vanadium | 86.382 | 0.265 | 77.764 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 12

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 13.512 | 0.271 | 22.080 |
| Vanadium | 86.488 | 0.271 | 77.920 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 13

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 13.920 | 0.269 | 22.679 |
| Vanadium | 86.080 | 0.269 | 77.321 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 14

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 4.360 | 0.187 | 7.637 |
| Vanadium | 95.640 | 0.187 | 92.363 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 15

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 4.253 | 0.187 | 7.456 |
| Vanadium | 95.747 | 0.187 | 92.544 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 16

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 3.933 | 0.182 | 6.913 |
| Vanadium | 96.067 | 0.182 | 93.087 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 17

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 6.971 | 0.218 | 11.966 |
| Vanadium | 93.029 | 0.218 | 88.034 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 18

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 6.716 | 0.213 | 11.550 |
| Vanadium | 93.284 | 0.213 | 88.450 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 19

Electron Image

Image Width: 164.0 µm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 7.569 | 0.219 | 12.932 |
| Vanadium | 92.431 | 0.219 | 87.068 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 10.035 | 0.236 | 16.827 |
| Vanadium | 89.965 | 0.236 | 83.173 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  14.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 10.084 | 0.259 | 16.904 |
| Vanadium | 89.916 | 0.259 | 83.096 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  15.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 9.918 | 0.262 | 16.646 |
| Vanadium | 90.082 | 0.262 | 83.354 |