Spectrum details

Project	New project 	Spectrum name	Spectrum 9

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.078 | 0.322 | 66.342 |
| Vanadium | 47.922 | 0.322 | 33.658 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 8

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.379 | 0.330 | 66.611 |
| Vanadium | 47.621 | 0.330 | 33.389 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 7

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.203 | 0.327 | 66.454 |
| Vanadium | 47.797 | 0.327 | 33.546 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.531 | 0.285 | 46.654 |
| Vanadium | 67.469 | 0.285 | 53.346 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.532 | 0.290 | 46.655 |
| Vanadium | 67.468 | 0.290 | 53.345 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.525 | 0.286 | 46.647 |
| Vanadium | 67.475 | 0.286 | 53.353 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 27.865 | 0.272 | 41.198 |
| Vanadium | 72.135 | 0.272 | 58.802 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 28.251 | 0.270 | 41.663 |
| Vanadium | 71.749 | 0.270 | 58.337 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 246.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 27.990 | 0.271 | 41.349 |
| Vanadium | 72.010 | 0.271 | 58.651 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 39.026 | 0.311 | 53.722 |
| Vanadium | 60.975 | 0.311 | 46.278 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 41.618 | 0.313 | 56.389 |
| Vanadium | 58.382 | 0.313 | 43.611 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 983.9 µm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 41.974 | 0.302 | 56.748 |
| Vanadium | 58.026 | 0.302 | 43.252 |