Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.764 | 0.341 | 66.954 |
| Vanadium | 47.236 | 0.341 | 33.046 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.540 | 0.346 | 66.754 |
| Vanadium | 47.460 | 0.346 | 33.246 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.329 | 0.343 | 66.566 |
| Vanadium | 47.671 | 0.343 | 33.434 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.624 | 0.302 | 46.759 |
| Vanadium | 67.376 | 0.302 | 53.241 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.582 | 0.301 | 46.712 |
| Vanadium | 67.418 | 0.301 | 53.288 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.878 | 0.302 | 47.046 |
| Vanadium | 67.122 | 0.302 | 52.954 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 47.633 | 0.324 | 62.261 |
| Vanadium | 52.367 | 0.324 | 37.739 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 3.280 mm

Acquisition conditions

Acquisition time (s)  19.8 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 47.580 | 0.326 | 62.211 |
| Vanadium | 52.420 | 0.326 | 37.789 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 3.280 mm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 46.844 | 0.373 | 61.515 |
| Vanadium | 53.156 | 0.373 | 38.485 |