Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 328.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 52.563 | 0.347 | 66.775 |
| Vanadium | 47.437 | 0.347 | 33.225 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 328.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 53.628 | 0.344 | 67.717 |
| Vanadium | 46.372 | 0.344 | 32.283 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 328.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 53.477 | 0.348 | 67.584 |
| Vanadium | 46.523 | 0.348 | 32.416 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 328.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 99.430 | 0.155 | 99.685 |
| Vanadium | 0.570 | 0.155 | 0.315 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 5

Electron Image

Image Width: 328.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 99.370 | 0.149 | 99.652 |
| Vanadium | 0.630 | 0.149 | 0.348 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 6

Electron Image

Image Width: 328.0 µm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 99.308 | 0.156 | 99.618 |
| Vanadium | 0.692 | 0.156 | 0.383 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.1 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 78.772 | 0.315 | 87.064 |
| Vanadium | 21.228 | 0.315 | 12.936 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  20.0 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 80.452 | 0.343 | 88.187 |
| Vanadium | 19.548 | 0.343 | 11.813 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 2.460 mm

Acquisition conditions

Acquisition time (s)  19.9 	Process time  5

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 78.702 | 0.364 | 87.017 |
| Vanadium | 21.298 | 0.364 | 12.983 |